# Electromigration (EM) Reliability Report

Document Version: 2.5.0
Date: 2025-01-15
Author: Semiconductor Reliability Team

# 1. Introduction

Electromigration (EM) is the transport of material caused by the gradual movement of metal atoms in a conductor due to momentum transfer between conducting electrons and diffusing metal atoms. It is a significant reliability concern in semiconductor devices, particularly as feature sizes shrink below 28nm technology nodes.

This report presents EM qualification data for our advanced interconnect technology, including MTTF (Mean Time To Failure) measurements at multiple temperature conditions. The data was collected following JEDEC standard JESD61 test methodology.

# 2. EM Physics and Background

Electromigration occurs when current density in a metal interconnect exceeds a critical threshold. The driving force is the 'electron wind' — momentum exchange between conduction electrons and metal ions. The phenomenon is described by Black's equation:

MTTF = A × (J)^(-n) × exp(Ea / kT)

Where A is a constant, J is current density, n is the current exponent (typically ~2), Ea is activation energy, k is Boltzmann's constant, and T is absolute temperature in Kelvin.

The DB stores all measurement data. The test setup uses a backend server to manage data collection. The frontend provides real-time monitoring.

Testing began on 2024/3/15 and completed on 24-06-30. Final review date: 2025-01-15.

# 3. Test Methodology

EM lifetime tests were performed using JEDEC standard JESD61 methodology. Samples were stressed at elevated temperatures (100°C to 350°C) with constant current density. The test structures include single-via chains and multi-via chains across all metal layers (M1 through M9).

## 3.1 Test Conditions

| Parameter | Value | Unit | Notes |
| --- | --- | --- | --- |
| Current Density | 1.5 | MA/cm² | Per JEDEC spec |
| Temperature Range | 100–350 | °C | 5 test points |
| Sample Size | 30 | units/condition | Statistical minimum |
| Failure Criterion | 10% | ΔR/R₀ | Resistance shift |
| Test Duration | 1000 | hours | Maximum stress time |

# 4. Test Structures

The following metal layers were characterized for EM performance. Each layer uses copper dual-damascene integration with TaN/Ta barrier.

| Metal Layer | Width (nm) | Thickness (nm) | Barrier | Cap Layer |
| --- | --- | --- | --- | --- |
| Metal 1 (M1) | 40 | 80 | TaN/Ta | SiCN |
| Metal 2 (M2) | 40 | 80 | TaN/Ta | SiCN |
| Metal 3 (M3) | 64 | 120 | TaN/Ta | SiCN |
| Metal 4 (M4) | 64 | 120 | TaN/Ta | SiCN |
| Metal 5 (M5) | 100 | 200 | TaN/Ta | SiCN |
| Metal 6 (M6) | 100 | 200 | TaN/Ta | SiCN |
| Metal 7 (M7) | 200 | 400 | TaN/Ta | SiCN |
| Metal 8 (M8) | 400 | 800 | TaN/Ta | SiCN |
| Metal 9 (M9) | 800 | 3200 | TaN/Ta | SiCN |

# 5. EM Lifetime Data

The following table presents normalized MTTF values across temperature conditions. Values are expected to decrease monotonically with increasing temperature per Black's equation (Arrhenius behavior).

## 5.1 MTTF Data — All Metal Layers

| Metal Layer | Temperature | 100°C | 150°C | 200°C | 250°C | 300°C |
| --- | --- | --- | --- | --- | --- | --- |
| Metal 1 (M1) | Stress | 12500 | 5200 | 1800 | 620 | 210 |
| Metal 2 (M2) | Stress | 11800 | 4900 | 1700 | 580 | 195 |
| Metal 3 (M3) | Stress | 15200 | 6400 | 2200 | 760 | 255 |
| Metal 4 (M4) | Stress | 14800 | 6100 | 2100 | 730 | 245 |
| Metal 5 (M5) | Stress | 18500 | 7800 | 4500 | 2700 | 2900 |
| Metal 6 (M6) | Stress | 18100 | 7600 | 4300 | 2600 | 870 |
| Metal 7 (M7) | Stress | 25000 | 10500 | 3600 | 1250 | 420 |
| Metal 8 (M8) | Stress | 35000 | 14700 | 5100 | 1760 | 590 |
| Metal 9 (M9) | Stress | 52000 | 21800 | 7500 | 2600 | 870 |

# 6. Activation Energy Analysis

Activation energy (Ea) was extracted from Arrhenius plots for each metal layer. The expected Ea for Cu interconnects ranges from 0.7 to 1.0 eV, depending on the dominant diffusion path (grain boundary vs. interface).

| Metal Layer | Ea (eV) | Diffusion Path | R² Value |
| --- | --- | --- | --- |
| Metal 1 (M1) | 0.85 | Interface | 0.998 |
| Metal 2 (M2) | 0.83 | Interface | 0.997 |
| Metal 3 (M3) | 0.88 | Interface | 0.999 |
| Metal 5 (M5) | 0.91 | Mixed | 0.995 |
| Metal 7 (M7) | 0.78 | Grain Boundary | 0.996 |
| Metal 9 (M9) | 0.75 | Grain Boundary | 0.994 |

# 7. Risk Assessment

The following table summarizes reliability risks identified during EM qualification. Each risk item is assessed for impact level and probability.

| Risk ID | Description | Impact Level | Probability | Mitigation |
| --- | --- | --- | --- | --- |
| R001 | M5 anomalous EM at 300°C | High | Medium | Re-test with larger sample |
| R002 | M7 grain boundary diffusion | Severe | Low | Monitor in production |
| R003 | Via chain weak link | Medium | High | Design rule update |
| R004 | Interface delamination risk | High | Medium |  |
| R005 | Joule heating at high J | Low | Low |  |

# 8. Current Density Guidelines

Based on the EM qualification data, the following maximum current density (Jmax) values are recommended for each metal layer at the specified operating conditions.

| Metal Layer | Jmax DC (MA/cm²) | Jmax AC (MA/cm²) | Condition |
| --- | --- | --- | --- |
| Metal 1 (M1) | 1.0 | 3.0 | 105°C, 10yr |
| Metal 2 (M2) | 1.0 | 3.0 | 105°C, 10yr |
| Metal 3 (M3) | 1.5 | 4.5 | 105°C, 10yr |
| Metal 5 (M5) | 2.0 | 6.0 | 105°C, 10yr |
| Metal 7 (M7) | 3.0 | 9.0 | 105°C, 10yr |
| Metal 9 (M9) | 5.0 | 15.0 | 105°C, 10yr |

# 9. Summary

Version: 2.5.0

The EM qualification results demonstrate that all metal layers meet the required reliability targets for 10-year product lifetime at 105°C operating conditions, with the exception of Metal 5 (M5) which shows an anomalous data point at 300°C requiring further investigation.

Key findings:
• All metal layers show activation energies in the range 0.75–0.91 eV
• Current density guidelines are established for DC and AC conditions
• One anomalous data point identified in M5 at 300°C (under review)
• Risk assessment identifies 5 items, with 2 requiring active mitigation

# 10. Reliability Rules

This chapter contains the detailed reliability qualification data tables. All cells in these tables must contain valid data — no empty values are permitted.

## 10.1 EM Qualification Summary

| Metal Layer | Temperature | 100°C MTTF (hrs) | 200°C MTTF (hrs) | 300°C MTTF (hrs) | Status |
| --- | --- | --- | --- | --- | --- |
| Metal 1 (M1) | Stress | 12500 | 1800 | 210 | PASS |
| Metal 2 (M2) | Stress | 11800 | 1700 | 195 | PASS |
| Metal 3 (M3) | Stress | 15200 |  | 255 |  |
| Metal 4 (M4) | Stress | 14800 | 2100 | 245 | PASS |
| Metal 5 (M5) | Stress | 18500 | 4500 | 2900 | FAIL |
| Metal 6 (M6) | Stress | 18100 | 4300 |  | PASS |

## 10.2 Via Chain Reliability

| Via Type | Sample Size | MTTF (hrs) | Sigma | Pass/Fail |
| --- | --- | --- | --- | --- |
| V1 (M1-M2) | 30 | 8500 | 1.2 | PASS |
| V2 (M2-M3) | 30 | 9200 | 1.1 | PASS |
| V3 (M3-M4) | 30 | 8800 | 1.3 | PASS |
| V4 (M4-M5) | 30 |  |  | PENDING |
| V5 (M5-M6) | 30 | 10500 | 0.9 | PASS |

# Appendix A: References

1. JEDEC Standard JESD61 — Isothermal Electromigration Test Procedure
2. Black, J.R. (1969). Electromigration — A Brief Survey and Some Recent Results. IEEE Transactions on Electron Devices, 16(4), 338-347.
3. JEDEC Standard JEP154 — Guideline for Characterizing Solder Bump Electromigration
4. I. A. Blech (1976). Electromigration in thin aluminum films on titanium nitride. Journal of Applied Physics, 47(4), 1203-1208.